## Slide 1
The Charge Transfer Multiplet program
Introduction: Why Charge transfer and Multiplets?
Chapter 1: ATOMIC MULTIPLETS (9-10)
Chapter 2: CRYSTAL FIELD EFFECTS (10-11)
Chapter 3: CHARGE TRANSFER (13-14)
Chapter 4: X-MCD (15-16)
Chapter 5: PHOTOEMISSION AND AUGER (15-16)
Chapter 6: X-RAY EMISSION AND RIXS (15-16)

## Slide 2
Hocking et al. (JACS, 128, 10442)
The Charge Transfer Multiplet program

## Slide 3
Core Level Spectroscopies

## Slide 4
Excitations of core electrons to empty states
The XAS spectrum is given by the Fermi Golden Rule
X-ray Absorption Spectroscopy

## Slide 5
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
Single electron (excitation) approximation:
IXAS = |<empty|dipole| core>|2 
Neglect <vv’|1/r|vv’> (‘many body effects’)
Neglect <cv|1/r|cv> (‘multiplet effects’)
X-ray Absorption Spectroscopy

## Slide 6
Element specific DOS
L specific DOS
Dipole selection rule (L= ±1)
oxide
1s
X-ray Absorption Spectroscopy

## Slide 7
Phys. Rev. B.
40, 5715 (1989) / 48, 2074 (1993)
TiO2 (rutile)
TiO2 (anatase)
Element specific DOS
L specific DOS
Core hole effects
Multiplet effects
Many body effects
X-ray Absorption Spectroscopy

## Slide 8
XAS probes empty DOS
Core Hole pulls down DOS
Final State Rule: Spectral shape of XAS looks like final state DOS
Initial State Rule: Intensity of XAS is given by the initial state
Phys. Rev. B.
41, 11899 (1991)
Dipole selection rule (L= ±1)
Element specific DOS
L specific DOS
TiSi2
XAS: core hole effect

## Slide 9
2p3/2
2p1/2
Multiplet effect: Strong overlap of 2p-core and 3d-valence wave functions
Single Particle model breaks down:
Necessary to use atomic-like configurations.
Charge Transfer: Core hole potential causes reordering of configurations
3d
<pd|1/r|pd>
~ 10 eV
XAS: multiplets and charge transfer

## Slide 10
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS

## Slide 11
Spectral shape determined by:
  (1) Multiplet effects
  (2) Charge Transfer
J. Elec. Spec.
67, 529 (1994)
Charge transfer effects in XAS and XPS

## Slide 12
Spectral shape determined by:
  (1) Multiplet effects
  (2) Charge Transfer
Relative Energy (eV)
NiBr2
NiO
J. Elec. Spec.
67, 529 (1994)
Charge transfer effects in XAS and XPS

## Slide 13
Single Electron Excitation:
K edges
(WIEN, FEFF, ….)
Many Body Excitation:
Other edges
(CTM)
X-ray Absorption Spectroscopy

## Slide 14
Single Electron Excitation:
K main edge
(WIEN, FEFF, ….)
Many Body Excitation:
Other edges
+K pre-edge
(CTM)
No Unified Interpretation!
X-ray Absorption Spectroscopy

## Slide 15
Chapter 1: ATOMIC MULTIPLETS
3d and 4d XAS of La3+ ions
Term symbols
XAS described with Atomic Multiplets.
2p XAS of TiO2
Atomic multiplet ground states of 3dn systems
Using the CTM program

## Slide 16
2S+1L
L Azimuthal quantum number L= |l1-l2|, |l1-l2+1|, …l1+l2 3d: l=2 3d2: L=0,1,2,3,4
S Spin quantum number S= |s1-s2|, |s1-s2+1|, …s1+s2 3d: s=1/2 3d2: S=0,1
mL magnetic quantum number mL=-L, L+1, …L 3d: ml=2,1,0,-1,-2
mS spin magnetic quantum number mS=-S, S+1,…, S 3d: ms=1/2, -1/2 (,)
Term Symbols (LS)

## Slide 17
2S+1LJ
J Spin quantum number J= |L-S|, |L-S+1|, …, L+S 3d: j=3/2,5/2 3d2: j=0,1,2,3,4
Not all combinations of L+S are possible!
mJ total magnetic quantum number mJ=-J, J+1, …J
3d5/2: mj=5/2,3/2,1/2,-1/2,-3/2,-5/2
Term Symbols (LSJ)

## Slide 18
ML=4
MS=0
MJ=4
Term Symbols
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 
ML=3
MS=1
MJ=4

## Slide 19
Configurations of 2p2
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 
1  | 0  | -1 

## Slide 20
LS term symbols: 1S, 1D, 3P
LSJ term symbols:
 | MS=1 | MS=0 | MS=-1
ML= 2 | 0 | 1 | 0
ML= 1 | 1 | 2 | 1
ML= 0 | 1 | 3 | 1
ML=-1 | 1 | 2 | 1
ML=-2 | 0 | 1 | 0
Term Symbols of 2p2
1S0 1D2 3P0 3P1 3P2

## Slide 21
Determine term symbols of all partly filled shells
Multiply term symbols of different shells
2P2D gives 1,3P,D,F
S1=1/2, S2=1/2 >> S=0 or 1
L1 = 1, L2 = 2 >> L=3 or 2 or 1
Term Symbols

## Slide 22
    Determine term symbol of ground state
    maximum S
    maximum L
    maximum J (if shell is more than half-full)
    3d1 has 2D3/2 ground state 3d2: 3F2
    3d9 has 2D5/2 ground state 3d8: 3F4
Hund’s rules

## Slide 23
3d XAS of La2O3
La in La2O3 can be described as La3+ ions:
Ground state is 4f0
Dipole transition 4f03d94f1
Ground state symmetry: 1S0
Final state symmetry: 2D2F gives
1P, 1D, 1F, 1G, 1H and 3P, 3D, 3F, 3G, 3H.

## Slide 24
3d XAS of La2O3
Final state symmetries: 1P, 1D, 1F, 1G, 1H and 3P, 3D, 3F, 3G, 3H.
Transition <1S0|J=+1| 1P1, 3P1 , 3D1>
3 peaks in the spectrum

## Slide 25
3d XAS of La2O3
als2la3.rcg
als2la3.plo
als2la3.org
rcg2 als2la3
plo2 als2la3
als2la3.ps

## Slide 26
als2la3.rcg
10 1 0 00 4 4 1 1 SHELL00000000 SPIN00000000 INTER8
0 80998080 8065.47800 0000000
1 2 1 12 1 10 00 9 00000000 0 8065.4790 .00 1
D10 S 0
D 9 F 1
La3+ 3D10 4F00 1 0.0000 0.0000 0.0000 0.0000 0.0000HR99999999
La3+ 3D09 4F01 8 841.4990 6.7992 0.0922 7.0633 3.1673HR99999999
4.7234 2.7614 1.9054
La3+ 3D10 4F00 Dy3+ 3D09 4F01 -0.24802( 3D//R1// 4F) 1.000HR 34-100
-99999999.
-1
Run als2la3.rcg with rcg2 als2la3
3d XAS of La2O3

## Slide 27
als2la3.org
NO. OF LINES
J JP J-JP TOTAL KLAM ILOST
0.0 1.0 3 3 3000 0
1 ELEC DIP SPECTRUM (ENERGIES IN UNITS OF 8065.5 CM-1 = 1.00 EV)
1 DY3+ 3D10 4F00 --- DY3+ 3D09 4F01
0 E J CONF EP JP CONFP DELTA E LAMBDA(A) S/PMAX**2 GF LOG GF GA(SEC-1) CF,BRNCH
1 0.0000 0.0 1 (1S) 1S 833.2133 1.0 1 (2D) 3P 833.2133 14.8804 0.00690+ 0.0087 -2.062 2.611E+11 1.0000
2 0.0000 0.0 1 (1S) 1S 837.4330 1.0 1 (2D) 3D 837.4330 14.8054 0.80480+ 1.0157 0.007 3.091E+13 1.0000
3 0.0000 0.0 1 (1S) 1S 854.0414 1.0 1 (2D) 1P 854.0414 14.5175 1.18829+ 1.5294 0.185 4.840E+13 1.0000
3d XAS of La2O3

## Slide 28
als2la3.plo
1 postscript la3.ps
2 portrait
3 energy_range 830 865
4 columns_per_page 1
5 rows_per_page 2
6 frame_title La 3dXAS
7 lorentzian 0.2 999. range 0 845
8 lorentzian 0.4 9. range 845 999
9 gaussian 0.25
10 rcg9 la3.org
11 spectrum
12 end
3d XAS of La2O3

## Slide 29
3d XAS of La2O3

## Slide 30
3d XAS of La2O3
Thole et al.
PRB 32, 5107 (1985)

## Slide 31
    NdIII ion in Nd metal
    Ground state: 4f3
    Final state: 3d94f4
Thole et al.
PRB 32, 5107 (1985)
3d XAS of Nd

## Slide 32
2p XAS of TiO2

## Slide 33
    TiIV ion in TiO2:
    Ground state: 3d0
    Final state: 2p53d1
    Dipole transition: p-symmetry
    3d0-configuration: 1S, j=0 2p13d9-configuration: 2P2D = 1,3PDF j’=0,1,2,3,4
    p-transition: 1P j=+1,0,-1
    ground state symmetry: 1S 1S0
    transition: 1S 1P = 1P
    two possible final states: 1P 1P1,3P1,3D1,
2p XAS of TiO2

## Slide 34
2p XAS of TiO2
als3ti4.rcg
als3ti4.plo
als3ti4.org
rcg2 als3ti4
plo2 als3ti4
als3ti4.ps
als3ti4.rcn
als3ti4.rcf
rcn2 als3ti4
rename

## Slide 35
als3ti4.rcn
22 -9 2 10 1.0 5.E-06 1.E-09-2 130 1.0 0.65 0.0 0.50 0.0 .70
22 Ti4+ 2p06 3d00 2P06 3D00
22 Ti4+ 2p05 3d01 2P05 3D01
-1
Run als3ti4.rcn with rcn2 als3ti4 gives als3ti4.rcf
Only input:
atomic number
configurations
2p XAS of TiO2

## Slide 36
als3ti4.rcf
10 1 0 00 4 4 1 1 SHELL00000000 SPIN00000000 INTER8
0 80998080 8065.47800 0000000
1 2 1 12 1 10 00 9 00000000 0 8065.4790 .00 1
P 6 S 0
P 5 D 1
Ti4+ 2p06 3d00 1 0.0000 0.0000 0.0000 0.0000 0.0000HR99999999
Ti4+ 2p05 3d01 6 464.8110 3.7762 0.0322 6.3023 4.6284HR99999999
2.6334
Ti4+ 2p06 3d00 Ti4+ 2p05 3d01 -0.26267( 2P//R1// 3D) 1.000HR 38-100
-99999999.
-1
2p XAS of TiO2
Change 9 to 6
to print out the energy matrix and eigen vectors

## Slide 37
All final state interactions to zero
10 1 0 00 4 4 1 1 SHELL00000000 SPIN00000000 INTER8
0 80998080 8065.47800 0000000
1 2 1 12 1 10 00 9 00000000 0 8065.4790 .00 1
P 6 S 0
P 5 D 1
Ti4+ 2p06 3d00 1 0.0000 0.0000 0.0000 0.0000 0.0000HR99999999
Ti4+ 2p05 3d01 6 464.8110 0.0002 0.0002 0.0003 0.0004HR99999999
0.0004
Ti4+ 2p06 3d00 Ti4+ 2p05 3d01 -0.26267( 2P//R1// 3D) 1.000HR 38-100
-99999999.
-1
2p XAS of TiO2
Change to 0.000

## Slide 38
3d0 XAS calculation
0

## Slide 39
als3ti4a.org (all zero)
1 ENERGY MATRIX ( LS COUPLING) J= 1.0
1 1 1
(2P) 3D (2P) 3P (2P) 1P (
1 2 3
1 (2P) 3D 1 464.811 0.000 0.000
1 (2P) 3P 2 0.000 464.811 0.000
1 (2P) 1P 3 0.000 0.000 464.811
2p XAS of TiO2
EIGENVECTORS ( LS COUPLING)
1 P05 3D P05 3D P05 3D
(2P) 3D (2P) 3P (2P) 1P (
1 (2P) 3D 1 1.00000 0.00000 0.00000
1 (2P) 3P 2 0.00000 1.00000 0.00000
1 (2P) 1P 3 0.00000 0.00000 1.00000

## Slide 40
Include 2p spin-orbit coupling (+LS2p)
10 1 0 00 4 4 1 1 SHELL00000000 SPIN00000000 INTER8
0 80998080 8065.47800 0000000
1 2 1 12 1 10 00 9 00000000 0 8065.4790 .00 1
P 6 S 0
P 5 D 1
Ti4+ 2p06 3d00 1 0.0000 0.0000 0.0000 0.0000 0.0000HR99999999
Ti4+ 2p05 3d01 6 464.8110 3.7762 0.0002 0.0003 0.0004HR99999999
0.0004
Ti4+ 2p06 3d00 Ti4+ 2p05 3d01 -0.26267( 2P//R1// 3D) 1.000HR 38-100
-99999999.
-1
2p XAS of TiO2
Change back to 3.776

## Slide 41
3d0 XAS calculation
0
+LS2p

## Slide 42
als3ti4b.org (+LS2p)
1 ENERGY MATRIX ( LS COUPLING) J= 1.0
(2P) 3D (2P) 3P (2P) 1P (
1 2 3
1 (2P) 3D 1 465.755 1.635 2.312
1 (2P) 3P 2 1.635 463.867 1.335
1 (2P) 1P 3 2.312 1.335 464.811
2p XAS of TiO2
EIGENVECTORS ( LS COUPLING)
1 P05 3D P05 3D P05 3D
(2P) 1P (2P) 3P (2P) 3D (
1 (2P) 3D 1 -0.67098 0.22312 -0.70711
1 (2P) 3P 2 0.12977 -0.90360 -0.40826
1 (2P) 1P 3 0.73003 0.36569 -0.57734
0 EIGENVALUES (J= 1.0)
462.923 462.923 468.587
E=5.664 = 3/2*LS2p
0.730032+0.365692=0.6666
-0.577342=0.3333

## Slide 43
Include Slater-integrals (+FK, GK)
10 1 0 00 4 4 1 1 SHELL00000000 SPIN00000000 INTER8
0 80998080 8065.47800 0000000
1 2 1 12 1 10 00 9 00000000 0 8065.4790 .00 1
P 6 S 0
P 5 D 1
Ti4+ 2p06 3d00 1 0.0000 0.0000 0.0000 0.0000 0.0000HR99999999
Ti4+ 2p05 3d01 6 464.8110 0.0002 0.0002 6.3023 4.6284HR99999999
2.6334
Ti4+ 2p06 3d00 Ti4+ 2p05 3d01 -0.26267( 2P//R1// 3D) 1.000HR 38-100
-99999999.
-1
2p XAS of TiO2
Set the spin-orbit couplings to zero

## Slide 44
3d0 XAS calculation
0
+LS2p
+FK, GK

## Slide 45
als3ti4c.org (+FK, GK)
1 ENERGY MATRIX ( LS COUPLING) J= 1.0
(2P) 3D (2P) 3P (2P) 1P (
1 2 3
1 (2P) 3D 1 465.482 0.000 0.000
1 (2P) 3P 2 0.000 463.466 0.000
1 (2P) 1P 3 0.000 0.000 468.402
2p XAS of TiO2
EIGENVECTORS ( LS COUPLING)
1 P05 3D P05 3D P05 3D
(2P) 3P (2P) 3D (2P) 1P (
1 (2P) 3D 1 0.00000 1.00000 0.00000
1 (2P) 3P 2 1.00000 0.00000 0.00000
1 (2P) 1P 3 0.00000 0.00000 1.00000
0 EIGENVALUES (J= 1.0)
463.466 465.482 468.402

## Slide 46
Include LS2p,FK + GK
10 1 0 00 4 4 1 1 SHELL00000000 SPIN00000000 INTER8
0 80998080 8065.47800 0000000
1 2 1 12 1 10 00 9 00000000 0 8065.4790 .00 1
P 6 S 0
P 5 D 1
Ti4+ 2p06 3d00 1 0.0000 0.0000 0.0000 0.0000 0.0000HR99999999
Ti4+ 2p05 3d01 6 464.8110 3.7762 0.0002 6.3023 4.6284HR99999999
2.6334
Ti4+ 2p06 3d00 Ti4+ 2p05 3d01 -0.26267( 2P//R1// 3D) 1.000HR 38-100
-99999999.
-1
2p XAS of TiO2
Only the 3d spin-orbit coupling is zero

## Slide 47
als3ti4d.org (+LS2p +FK, GK)
1 ENERGY MATRIX ( LS COUPLING) J= 1.0
(2P) 3D (2P) 3P (2P) 1P (
1 2 3
1 (2P) 3D 1 466.426 1.635 2.312
1 (2P) 3P 2 1.635 462.522 1.335
1 (2P) 1P 3 2.312 1.335 468.402
2p XAS of TiO2
EIGENVECTORS ( LS COUPLING)
1 P05 3D P05 3D P05 3D
(2P) 3P (2P) 3D (2P) 1P (
1 (2P) 3D 1 0.29681 -0.77568 0.55698
1 (2P) 3P 2 -0.95074 -0.18539 0.24845
1 (2P) 1P 3 0.08946 0.60328 0.79250
0 EIGENVALUES (J= 1.0)
461.886 465.019 470.446

## Slide 48
3d0 XAS calculation
0
+LS2p
+FK, GK
+LS2p
+FK, GK

## Slide 49
3d0 XAS experiment (SrTiO3)

## Slide 50
3dN XAS calculation
Transition
Ground
Transitions
Term Symbols
3d02p53d1
1S0
3
12
3d12p53d2
2D3/2
29
45
3d22p53d3
3F2
68
110
3d32p53d4
4F3/2
95
180
3d42p53d5
5D0
32
205
3d52p53d6
6S5/2
110
180
3d62p53d7
5D2
68
110
3d72p53d8
4F9/2
16
45
3d82p53d9
3F4
4
12
3d92p53d10
2D5/2
1
2

## Slide 51
Term Symbols and XAS
    TiIV ion in TiO2:
    Ground state: 3d0
    Final state: 2p53d1
    Dipole transition: p-symmetry
    3d0-configuration: 1S, j=0 2p13d9-configuration: 2P2D = 1,3PDF j’=0,1,2,3,4
    p-transition: 1P j=+1,0,-1
    ground state : 1S 1S0
    transition: 1S 1P = 1P
    Allowed final states: 1P 1P1,3P1,3D1,

## Slide 52
    NiII ion in NiO:
    Ground state: 3d8
    Final state: 2p53d9
    Dipole transition: p-symmetry
    3d8-configuration: 1S, 1D, 3P,1G, 3F j=4 2p53d9-configuration: 2P2D = 1,3PDF j’=0,1,2,3,4
    p-transition: 1P j=+1,0,-1
    ground state : 3F 3F4
    transition: 3F 1P = 3DFG
    Allowed final states: 3D, 3F 3D3,3F3,3F4, 1F3
Term Symbols and XAS

## Slide 53
Atomic multiplet calculations for Ni2+
als3ni2a.rcg
all initial and final state interactions set to zero
als3ni2b.rcg
only the 2p spin-orbit coupling (LS2p) is included
als3ni2c.rcg
LS2p and the Slater-Condon parameters are included
als3ni2d.rcg
Also 3d spin-orbit coupling is added in the initial state. This yields the full Ni2+ calculation.

## Slide 54
3d8 XAS calculation
+LS2p
0
+FK, GK: > 3F
+LS3d : > 3F4

## Slide 55
Atomic multiplets