## Slide 1
(Resonant) Photoemission and Auger
2p-XPS
<3d8 | r |2p5 3d8 >
3s-XPS
<3d8 | r |3s1 3d8 >
2p3s3s-Res. Auger
<3d8 | r |2p5 3d9>
+ <2p5 3d9|1/r|3s03d9 >
2p3d3d-Res. Auger
<3d8 | r |2p5 3d9>
+ <2p5 3d9|1/r|3d7 >
 Resonant photoemission

## Slide 2
Photoemission and Auger

## Slide 3
3d8
3d9L
2p53d8
dipole
dipole
2p53d9L
Mixing t
Mixing t’
2p XPS (2 conf.)

## Slide 4
2p3s3s Res. Auger (2 conf.)
3d8
3d9L
2p53d9
AES
3s03d9
dipole
dipole
Mixing t
Mixing t’
2p53d10L
AES
3s03d10L

## Slide 5
Photoemission and Auger
XPS dipole transition (r)
<3d8 | r |2p5 3d8 >
Auger Coulomb operator (1/r)
<3p3p |1/r |2p  >

## Slide 6
3d8
3d9L
2p53d8
dipole
dipole
2p53d9L
Mixing t
Mixing t’
Mixing t
Mixing t’
3d10L2
dipole
2p53d10L2
2p XPS (3 conf.)

## Slide 7
Photoemission (2p XPS)

## Slide 8
als8ni2xps3.rcg
0 90999090 8065.47900 000000
10 14 0 0 1 1 INTER0
1 3 1 13 1 10 00 9 00000000 0 8065.4790 .00 1
D08 P06 D00
D08 P05 D01
Ni3+ 1 1
Ni3+ 2 1
-99999999.
Photoemission (2p XPS)
D08 P05 D01 = 3d8 2p5 d

## Slide 9
als8ni2xps3.rcg
0 80998080 8065.47900 000000
10 14 0 4 0 4 SHELL30000000 SPIN30000000 INTER2
1 3 1 13 1 10 00 9 00000000 0 8065.4790 .00 1
D08 P06 D10
D09 P06 D09
Ni3+P6D8L 4 0.0000 12.2341 7.5981 0.0832 0.0000HR99999999
Ni3+P6D9L2 2 0.0000 0.0742 0.0000 0.0000 0.0000HR99999999
-99999999.
0 80998080 8065.47900 000000
10 14 0 4 0 4 SHELL30000000 SPIN30000000 INTER2
1 3 1 13 1 10 00 9 00000000 0 8065.4790 .00 1
D09 P06 D09
D10 P06 D08
Ni3+P6D9L2 2 0.0000 0.0742 0.0000 0.0000 0.0000HR99999999
Ni3+P6D9L2 2 0.0000 0.0002 0.0000 0.0000 0.0000HR99999999
-99999999.
Photoemission (2p XPS)

## Slide 10
als8ni2xps3.rcg
10 14 0 4 0 4 SHELL30000000 SPIN30000000 INTER2
1 4 1 14 1 10 00 9 00000000 0 8065.4790 .00 1
D08 P05 D10 D01
D09 P05 D09 D01
Ni3+P5D8 8 862.3000 14.0221 8.7641 00.1122 11.5062HR99999999
8.3503 6.3324 3.6034
Ni3+P5D9L 6 862.3000 00.1022 11.5072 7.7213 5.7874HR99999999
3.2914
-99999999.
0 80998080 8065.47900 000000
10 14 0 4 0 4 SHELL30000000 SPIN30000000 INTER2
1 4 1 14 1 10 00 9 00000000 0 8065.4790 .00 1
D09 P05 D09 D01
D10 P05 D08 D01
Ni3+P5D9L 6 862.3000 00.1022 11.5072 7.7213 5.7874HR99999999
3.2914
Ni3+P5D10L2 2 862.3000 11.5092 0.0000 0.0000 0.0000HR99999999
-99999999.
Photoemission (2p XPS)

## Slide 11
als8ni2xps3.ban
NCONF 3 3
N2 1
N3 1
def EG1 = 0.0 unity
def EF1 = 0.0 unity
def EG2 = 3.5 unity
def EF2 = -5.0 unity
def EG3 = 14.0 unity
def EF3 = -3.0 unity
XMIX 4 3. 3. 1.5 1.5
2 1 1 2 1 2 3
XMIX 4 3. 3. 1.5 1.5
2 2 1 2 2 2 3
XHAM 4 1.0 1.0 0.0 0.0
6 1 1 1 2 1 3 2 1 2 2 2 3
TRAN 3 1 1 2 2 3 3
TRIADS
Photoemission (2p XPS)

## Slide 12
als8ni23sxps.rcg
0 80998080 8065.47800 0000000
10 14 0 4 0 4 INTER2 shell03000000
1 4 1 14 1 10 00 9 00000000 8065.4780 .00 0 1
S01 D09 D09 P01
S01 D10 D08 P01
Ni2+ 3s1 3d9 p 3 110.0000 .0852 12.8804 .0000 0.0000HR99999999
Ni2+ 3s1 3d10p 1 110.0000 .0000 00.0004 .0000 0.0000HR99999999
-99999999.
Photoemission (3s XPS)
S01 D09 D09 P01 = 3s1 3d9 L d

## Slide 13
Photoemission (2p XPS)
T=1
No mixing
T=2
T=3

## Slide 14
2p and 3s XPS
2pXPS
3sXPS
broad
broad

## Slide 15
Photoemission (2p XPS)
J. Phys. Soc. Japan.
61, 449 (1992)

## Slide 16
Photoemission (2p XPS)
J. Phys. Soc. Japan.
61, 449 (1992)

## Slide 17
Photoemission (2p XPS)
Phys. Rev. B.
59, 3195 (1999)

## Slide 18
all electrons
partly filled
direct XPS
ground state
2p63s23p63d8
3d8
-
2p core hole
(resonant)
2p53s23p63d9
2p53d9
-
2p3s3s Auger
2p63s03p63d9 + 
(3s0) 3d9
no
2p3s3p Auger
2p63s13p53d9 + 
3s13p53d9
no
2p3p3p Auger
2p63s23p43d9 + 
3p43d9
no
2p3s3d Auger
2p63s13p63d8 + 
3s13d8
3s XPS
2p3p3d Auger
2p63s23p53d8 + 
3p53d8
3p XPS
2p3d3d Auger
2p63s23p63d7 + 
3d7
3d XPS
Resonant Photoemission and Auger

## Slide 19
2p X-ray absorption

## Slide 20
2p3s3s resonant Auger

## Slide 21
2p X-ray absorption

## Slide 22
2p3s3s resonant Auger

## Slide 23
2p X-ray absorption

## Slide 24
2p3s3s resonant Auger

## Slide 25
2p X-ray absorption

## Slide 26
2p3s3s resonant Auger

## Slide 27
als9pssp.rcg
10 0 0 14 0 0 1 1 SPIN00000000 SHELL00000000 INTER0
0 8099808027 8065.47800 0000000
1 4 1 14 2-10 00 9 00000000 0 8065.4790 .00 1
P 6 S 2 D 8 P 0
P 5 S 2 D 9 P 0
P 6 S 0 D 9 P 1
Ni2+ 3d8
Ni2+ 2p5 3d9
Ni2+ 3s0 3d9 p
p5 3d09 -s0 3d9 p
-99999999.
2p3s3s resonant Auger

## Slide 28
als9pssp.rcg
10 0 0 14 4 4 0 4 SPIN00000000 SHELL00300000 INTER3
0 8099808027 8065.47800 0000000
1 5 2-15 2-10 00 9 00000000 0 8065.4790 .00 1
P 5 S 2 D 9 D10 p 0
P 6 S 0 D 9 D10 p 1
P 5 S 2 D10 D 9 p 0
P 6 S 0 D10 D 9 p 1
Ni2+ 2p5 3d09 6 .0000 11.5072 .0002 7.7213 5.7874HR99999999
3.2914
Ni2+ 3s0 3d9 p 6 1000.0000 .0942 .0002 .0003 .0004HR99999999
p5 3d09 -s0 3d9 p 1 .19665 .00005 .00005 .00005 .00005HR99999999
Ni2+ 2p5 3d10 2 0.0000 11.5092 .0000 .0000 .0000HR99999999
Ni2+ 3s0 3d10p 2 1000.0000 .0002 .0000 .0000 .0000HR99999999
p5 3d10 -s0 3d10p 1 .19275 .00005 .00005 .00005 .00005HR99999999
-99999999.
2p3s3s resonant Auger

## Slide 29
2p3s3s Res. Auger (2 conf.)
3d8
3d9L
2p53d9
AES
3s03d9
dipole
dipole
Mixing t
Mixing t’
2p53d10L
AES
3s03d10L

## Slide 30
als9pssp.rcg
10 0 0 14 4 4 0 4 SPIN00000000 SHELL00300000 INTER3
0 8099808027 8065.47800 0000000
1 5 2-15 2-10 00 9 00000000 0 8065.4790 .00 1
P 5 S 2 D 9 D10 p 0
P 6 S 0 D 9 D10 p 1
P 5 S 2 D10 D 9 p 0
P 6 S 0 D10 D 9 p 1
Ni2+ 2p5 3d09 6 .0000 11.5072 .0002 7.7213 5.7874HR99999999
3.2914
Ni2+ 3s0 3d9 p 6 1000.0000 .0942 .0002 .0003 .0004HR99999999
p5 3d09 -s0 3d9 p 1 .19665 .00005 .00005 .00005 .00005HR99999999
Ni2+ 2p5 3d10 2 0.0000 11.5092 .0000 .0000 .0000HR99999999
Ni2+ 3s0 3d10p 2 1000.0000 .0002 .0000 .0000 .0000HR99999999
p5 3d10 -s0 3d10p 1 .19275 .00005 .00005 .00005 .00005HR99999999
-99999999.
2p3s3s resonant Auger

## Slide 31
als9pssp.rcg
Ni2+ 2p5 3d09 6 .0000 11.5072 .0002 7.7213 5.7874HR99999999
3.2914
Ni2+ 3s0 3d9 p 6 1000.0000 .0942 .0002 .0003 .0004HR99999999
p5 3d09 -s0 3d9 p 1 .19665 .00005 .00005 .00005 .00005HR99999999
2p3s3s resonant Auger
<3s3s|1/r|2pp >

## Slide 32
als9pssp.ban
NCONF 2 2
N2 1
def EG2 = 3.5 unity
def EF2 = 2.0 unity
XMIX 2 2.2 -1.1
1 1 1 2
XMIX 2 1.8 -0.9
1 2 1 2
XHAM 2 1.0 0.7
4 1 1 1 2 2 1 2 2
TRAN 2 1 1 2 2
DIP 1.83761
AUGER
GAMMA 0.3
NO 1 CI 1 DIP 0.0
DEF EF2 = -4.5 unity
NOMEGA 20 ESTART -5.0 ESTEP 0.5
ENDAUGER
TRIADS
2p3s3s resonant Auger
<3s3s|1/r|2pp >

## Slide 33
als9pssp.oba
TRANSFORMED MATRIX FOR TRIAD ( ^1+ 11- 1- ) (1* 13) DIM : 1 : 0 : 1 ACTOR MULTIPOLE
BRA/KET : -5.18101 -5.18056 -4.66663 -4.66229 -4.66200 -4.66185 0.21902
-3.52398: 0.000051 0.000010 0.000000 0.000000 0.000000 0.000000 0.000050
BRA/KET : 0.21954 0.21972 0.35318 0.53119 0.53131 0.53169
-3.52398: 0.000013 0.000000 0.000002 0.000001 0.000000 0.000000
Total intensity 0.00013
TRANSFORMED MATRIX FOR TRIAD ( ^1+ 21- 1- ) (1* 13) DIM : 1 : 0 : 1 ACTOR MULTIPOLE
BRA/KET : -5.18101 -5.18056 -4.66663 -4.66229 -4.66200 -4.66185 0.21902
-3.52398: 0.000196 0.000016 0.000002 0.000003 0.000000 0.000000 0.000207
BRA/KET : 0.21954 0.21972 0.35318 0.53119 0.53131 0.53169
-3.52398: 0.000026 0.000000 0.000011 0.000001 0.000000 0.000001
Total intensity 0.00046
-5.0
-4.5
2p3s3s resonant Auger
NOMEGA 20 ESTART -5.0 ESTEP 0.5

## Slide 34
2p3s3s resonant Auger

## Slide 35
als9pssp.oba
TRANSFORMED MATRIX FOR TRIAD ( ^1+ 11- 1- ) (1* 13) DIM : 1 : 0 : 1 ACTOR MULTIPOLE
BRA/KET : -5.18101 -5.18056 -4.66663 -4.66229 -4.66200 -4.66185 0.21902
-3.52398: 0.000051 0.000010 0.000000 0.000000 0.000000 0.000000 0.000050
BRA/KET : 0.21954 0.21972 0.35318 0.53119 0.53131 0.53169
-3.52398: 0.000013 0.000000 0.000002 0.000001 0.000000 0.000000
Total intensity 0.00013
TRANSFORMED MATRIX FOR TRIAD ( ^1+ 21- 1- ) (1* 13) DIM : 1 : 0 : 1 ACTOR MULTIPOLE
BRA/KET : -5.18101 -5.18056 -4.66663 -4.66229 -4.66200 -4.66185 0.21902
-3.52398: 0.000196 0.000016 0.000002 0.000003 0.000000 0.000000 0.000207
BRA/KET : 0.21954 0.21972 0.35318 0.53119 0.53131 0.53169
-3.52398: 0.000026 0.000000 0.000011 0.000001 0.000000 0.000001
Total intensity 0.00046
-5.0
-4.5
2p3s3s resonant Auger
NOMEGA 20 ESTART -5.0 ESTEP 0.5

## Slide 36
2p3s3s resonant Auger

## Slide 37
2p3s3s resonant Auger

## Slide 38
2p3s3p resonant Auger
d
s
Satellite

## Slide 39
Comparison with experiment
finazzi99a.pdf

## Slide 40
als9ni2p3s3p.rcn
22 -9 2 10 1.0 5.E-08 1.E-11-2 130 1.0 0.65 45.0 0.50 0.0 0.70
28 Ni2+ 3d8 3D08
28 Ni2+ 2p5 3d09 2P05 3D09
28 Ni2+ 3s1 3p5 3d9 s 3S01 3P05 3D0999S01 45.0
28 Ni2+ 3s1 3p5 3d9 d 3S01 3P05 3D0999D01 45.0
-1
Calculating Auger matrix elements
<3s3p|1/r|2ps >
<3s3p|1/r|2pd >
<3s3p|1/r|2pg > ??

## Slide 41
als9ni2p3s3p.rcn
22 -9 2 10 1.0 5.E-08 1.E-11-2 130 1.0 0.65 45.0 0.50 0.0 0.70
28 Ni2+ 3d8 3D08
28 Ni2+ 2p5 3d09 2P05 3D09
28 Ni2+ 3s1 3p5 3d9 s 3S01 3P05 3D0999S01 45.0
28 Ni2+ 3s1 3p5 3d9 d 3S01 3P05 3D0999D01 45.0
-1
Calculating Auger matrix elements
<3s3p|1/r|2ps >
Kinetic energy in Rydbergs

## Slide 42
als9ni2p3s3p.rcf
Ni2+ 3d8 4 0.0000 12.2341 7.5981 0.0832 0.0000HR99999999
Ni2+ 2p5 3d09 6 860.1660 11.5072 0.1022 7.7213 5.7874HR99999999
3.2914
Ni2+ 3s1 3p5 3d9s 11-9500.0000 1.4042 0.0942 14.3893 21.7354HR99999999
13.5824 0.0004 17.7844 10.8434 0.0004 0.0004
Ni2+ 3s1 3p5 3d9d 18-8500.0000 1.4042 0.0942 0.0002 14.3893HR99999999
0.0003 0.0003 0.0003 21.7354 13.5824 0.0004 17.7844
10.8434 0.0004 0.0004 0.0004 0.0004 0.0004
p5 3d09 -s1 3p5 3d2 0.19415 0.23675 0.00005 0.00005 0.00005HR99999999
p5 3d09 -s1 3p5 3d2 -0.01005 0.00615 0.00005 0.00005 0.00005HR99999999
s1 3p5 3d-s1 3p5 3d4 0.00005 0.00005 0.00005 0.00005 0.00005HR99999999
Ni2+ 3d8 Ni2+ 2p5 3d09 -0.18503( 2P//R1// 3D) 1.000HR 36-100
Ni2+ 3d8 Ni2+ 3s1 3p5 3d9 s 0.00000( //R1// ) 0.000HR 0 0
Ni2+ 3d8 Ni2+ 3s1 3p5 3d9 d 0.00000( //R1// ) 0.000HR 0 0
-99999999.
-1
Calculating Auger matrix elements

## Slide 43
Resonant vs. non-resonant Auger
2p3s3s-Res. Auger
<3d8 | r |2p5 3d9>
+ <2p5 3d9|1/r|3s03d9>
2p3s3s-non-res. Auger
<3d8 | r | 2p53d9 >
+<2p53d9|1/r|3s03d8’>

## Slide 44
Resonant vs. non-resonant Auger

## Slide 45
2p3d3d-Res. Auger
<3d8 | r |2p5 3d9>
+ <2p5 3d9|1/r|3d7 >
 Resonant photoemission
Resonant Photoemission

## Slide 46
martensson99a.pdf
Resonant Photoemission on Ni metal

## Slide 47
SP-CD Resonant Photoemission
tjeng97a.pdf

## Slide 48
SP-CD Resonant Photoemission
tjeng97a.pdf
A+ = 14, A- = 6, B+ = 1, B- = 3
MCD = A+ - A- + B+ - B- /  = 6/24 = 1/4
SPCD = A+ - A- - B+ + B- /  = 10/24 =5/12